SECTION 7 42 13

METAL WALL PANELS

PART 2 - PRODUCTS

- Panel Materials

- Aluminum Panels

- Material: Aluminum alloy 3003-H14

- Thickness: 0.040 inch minimum

- Finish: Kynar 500 fluoropolymer, 70% PVDF

- Steel Panels

- Material: G90 galvanized steel

- Thickness: 22 gauge minimum

2.05	ACCESSORIES

- Fasteners: Stainless steel, concealed type.

- Self-drilling screws with neoprene washers

- Blind rivets where indicated

- Sealant: Silicone, color to match panels

- Flashing: Same material and finish as panels

PART 1 - GENERAL

- Summary

- section includes:

- Factory-formed metal wall panels.

- Panel accessories and trim

- Sub-framing for panel attachment

- related sections

- Section 05 41 00 - Structural Metal Framing

- Section 07 92 00 - Joint Sealants

1.3	SUBMITTALS

- Product Data: Submit manufacturer's product data

- Include panel profiles and dimensions

- Include finish color charts

- Shop Drawings: Submit fabrication and installation drawings

- Samples: Submit 12 inch square samples of each panel type and color

1.3	QUALITY ASSURANCE

- Manufacturer Qualifications: Minimum 10 years experience.

- Installer Qualifications: Approved by panel manufacturer.

1.4	DELIVERY, STORAGE AND HANDLING

1.6	REFERENCES

- ASTM B209 - Aluminum Sheet

- AAMA 2605 - High Performance Coatings

- Install panels plumb and level within 1/8 inch in 10 feet.

PART 3 - EXECUTION

3.02	INSTALLATION

- Install panels per manufacturer's instructions and approved shop drawings.

- Align panels with building grid lines

- Maintain uniform joint widths

- Seal joints watertight with specified sealant.

- Coordinate with other trades for penetrations.

- Protect installed panels from damage.

- CLEANING

- Clean panel surfaces upon completion.

- Acceptable Manufacturers:

- CENTRIA

- ATAS International

- Metalwërks

- Remove protective film from panels.

- Touch up minor scratches with manufacturer's touch-up paint.

3.05	WARRANTY

A.	PROVIDE 20 YEAR WARRANTY ON PANEL FINISH

B.	PROVIDE 5 YEAR WARRANTY ON INSTALLATION

PART 2 - PRODUCTS (CONTINUED)

2.03	MANUFACTURERS

- See Article 3.03 for acceptable manufacturers.

END OF SECTON