SECTION 07 92 00

JOINT SEALANTS

PART 1 - GENERAL

- SUMMARY

- Section Includes:

- Joint sealants for interior and exterior applications.

- Joint fillers and backing materials.

- Surface preparation and priming.

- Related Sections:

- Section 07 84 00 - Firestopping.

- Section 08 80 00 - Glazing.

- REFERENCES

- Reference Standards:

- ASTM C920 - Standard Specification for Elastomeric Joint Sealants.

- ASTM C1193 - Standard Guide for Use of Joint Sealants.

- ASTM C1248 - Standard Test Method for Staining of Porous Substrate by Joint Sealants.

- SUBMITTALS

- Product Data: Submit manufacturer's technical data for each sealant product.

- Include product characteristics, performance criteria, and limitations.

- Include color charts for selection.

- Samples: Submit two samples of each sealant color specified.

- QUALITY ASSURANCE

- Installer Qualifications: Minimum 3 years documented experience.

- Single Source Responsibility: Obtain each type of sealant from single manufacturer.

PART 2 - PRODUCTS

- MANUFACTURERS

- Acceptable Manufacturers:

- Dow Corning Corporation.

- Pecora Corporation.

- Tremco Incorporated.

- Substitutions: In accordance with Section 01 60 00.

- MATERIALS

- Silicone Sealant (Type S-1): Single component, neutral cure silicone.

- Compliance: ASTM C920, Type S, Grade NS, Class 50, Use NT, M, G, A, O.

- Movement Capability: Plus or minus 50 percent.

- Color: As selected by Architect from manufacturer's standard colors.

- Polyurethane Sealant (Type P-1): Single component, moisture curing polyurethane.

- Compliance: ASTM C920, Type S, Grade NS, Class 25, Use T, M, A, O.

- Movement Capability: Plus or minus 25 percent.

- Interior applications only.

- Not for use in wet locations.

- Backer Rod: Closed-cell polyethylene foam, oversized 25 to 50 percent.

PART 3 - EXECUTION

- EXAMINATION

- Verify joint openings are ready to receive sealants.

- Joint widths and depths within tolerances specified.

- Joint surfaces are clean, dry, and free of contaminants.

- Do not proceed until unsatisfactory conditions are corrected.

- PREPARATION

- Surface Preparation:

- Clean joint surfaces of dust, dirt, oil, grease, and other contaminants.

- Use methods recommended by sealant manufacturer.

- Allow surfaces to dry completely before applying primer or sealant.

- Apply primer where required by sealant manufacturer.

- Install backer rod to achieve proper sealant depth-to-width ratio.

- APPLICATION

- Apply sealant in accordance with manufacturer's recommendations.

- Tool joints immediately after application for proper contact and appearance.

- Remove excess sealant and masking tape immediately after tooling.

- Protect installed sealants from damage until fully cured.

END OF SECTION