SECTION 09 29 00

GYPSUM BOARD

PART 1 - GENERAL

- SUMMARY

- Section Includes:

- Gypsum board assemblies for walls and ceilings.

- Non-load bearing metal framing for gypsum board assemblies.

- Joint treatment and finishing.

- Acoustical sealant at gypsum board assemblies.

- Related Sections:

- Section 05 40 00 - Cold-Formed Metal Framing.

- Section 09 91 00 - Painting.

- REFERENCES

- Reference Standards:

- ASTM C36 - Standard Specification for Gypsum Wallboard.

- ASTM C475 - Standard Specification for Joint Compound and Joint Tape.

- ASTM C645 - Standard Specification for Nonstructural Steel Framing Members.

- GA-216 - Application and Finishing of Gypsum Panel Products.

- SUBMITTALS

- Product Data:

- Submit manufacturer's product data for each type of gypsum board.

- Submit framing manufacturer's data including load tables.

- Shop Drawings: Submit details of edge conditions, control joints, and special assemblies.

- QUALITY ASSURANCE

- Fire-Resistance Ratings: Provide assemblies identical to those tested per ASTM E119.

- STC Ratings: Provide assemblies meeting or exceeding ratings indicated on Drawings.

PART 2 - PRODUCTS

- MANUFACTURERS

- Acceptable Manufacturers - Gypsum Board:

- USG Corporation.

- National Gypsum Company.

- Georgia-Pacific Gypsum LLC.

- Acceptable Manufacturers - Metal Framing:

- ClarkDietrich Building Systems.

- Marino\WARE.

- GYPSUM BOARD MATERIALS

- Standard Gypsum Board (Type X): Fire-rated, 5/8 inch thick.

- Compliance: ASTM C36, Type X.

- Core: Type X fire-resistant.

- Edges: Tapered on long edges.

- Application: Interior walls and ceilings requiring fire rating.

- Moisture-Resistant Gypsum Board: 5/8 inch thick.

- Compliance: ASTM C1396, moisture-resistant type.

- Water absorption: Maximum 5 percent by weight.

- Mold resistance: ASTM D3273, score of 10.

- Application: Toilet rooms, janitor closets, and similar wet areas.

- Abuse-Resistant Gypsum Board: 5/8 inch thick, impact resistant.

- Compliance: ASTM C1629, Level 3 abuse resistance.

- Application: Corridors, stairwells, and high-traffic areas.

- ACCESSORIES

- Joint Treatment Materials: Comply with ASTM C475.

- Joint tape, joint compound, and accessories from single manufacturer.

- Corner Beads: Galvanized steel or vinyl, as appropriate for location.

- Acoustical Sealant: Non-skinning, non-hardening, non-bleeding type.

PART 3 - EXECUTION

- EXAMINATION

- Verify framing is ready to receive gypsum board:

- Framing is plumb, level, and properly spaced.

- Blocking and backing are installed for wall-mounted items.

- MEP rough-in is complete and inspected.

- Environmental conditions: Maintain minimum 50°F and maximum 95°F.

- INSTALLATION

- Install gypsum board in accordance with GA-216 and manufacturer's instructions.

- Orient boards with long dimension perpendicular to framing.

- Stagger end joints minimum 12 inches between adjacent boards.

- Locate end joints over framing members.

- Do not align joints with corners of openings.

- Install screws per ASTM C1002 at spacing indicated on Drawings.

- Fire-rated assemblies: Install per tested assembly requirements.

- FINISHING

- Finish Level: As follows unless otherwise indicated:

- Level 4: Standard areas receiving paint or light wall covering.

- Embed tape in joint compound.

- Apply two separate coats of joint compound over tape.

- Apply one coat over fastener heads and accessories.

- Level 5: Critical lighting areas and surfaces receiving gloss paint.

- Sand joints smooth and remove dust before painting.

- PROTECTION

- Protect installed work from damage.

- Repair damaged surfaces to match adjacent work.

- Replace boards with unacceptable damage.

END OF SECTION