SECTION 09 30 00

CERAMIC TILING

PART 1 - GENERAL

- SUMMARY

- Section Includes:

- Ceramic tile for floors.

- Ceramic tile for walls.

- Porcelain tile for floors.

- Tile setting materials and grout.

- Related Sections:

- Section 07 92 00 - Joint Sealants.

- Section 09 91 00 - painting.

- REFERENCES

- Reference Standards:

- ANSI A108 - American National Standard Specifications for Installation of Ceramic Tile.

- ANSI A118 - American National Standard Specifications for Tile Installation Materials.

- ANSI A137.1 - American National Standard Specifications for Ceramic Tile.

- TCNA Handbook for Ceramic, Glass, and Stone Tile Installation.

- SUBMITTALS

- Product Data: Submit manufacturer's technical data for each tile and setting material.

- Include tile sizes, colors, and patterns.

- Include setting material specifications and limitations.

- Samples: Submit two full-size samples of each tile type and color.

- Grout samples to be submitted with tile samples.

- Shop Drawings: Submit tile layout drawings for patterned installations.

- Quality Assurance

- Installer Qualifications: Minimum 5 years experience with similar tile installations.

- Mock-Up: Construct mock-up of typical tile installation for Architect approval.

- Minimum 4 feet by 4 feet area.

- Include typical joints, corners, and transitions.

- DELIVERY, STORAGE, AND HANDLING

- Deliver materials in manufacturer's original packaging with labels intact.

- Store materials in dry location protected from weather.

- Condition materials to minimum 50 degrees F before installation.

PART 2 - PRODUCTS

- MANUFACTURERS

- Acceptable Manufacturers - Tile:

- Daltile.

- American Olean.

- Florida Tile Industries.

- Acceptable Manufacturers - Setting Materials:

- Laticrete International.

- MAPEI Corporation.

- Custom Building Products.

- TILE MATERIALS

- Floor Tile (Type FT-1): Porcelain, through-body color.

- Size: 12 inches by 12 inches by 3/8 inch thick.

- Finish: Matte, slip-resistant.

- DCOF: 0.42 minimum per ANSI A326.3.

- Color: As selected by Architect.

- Application: Toilet rooms, janitor closets, kitchen.

- Wall Tile (Type WT-1): Ceramic, glazed.

- Size: 4 inches by 4 inches by 5/16 inch thick.

- Finish: Gloss.

- Color: White.

- Accent Tile (Type AT-1): Glass mosaic.

- Size: 1 inch by 1 inch mounted on 12 inch by 12 inch sheets.

- SETTING MATERIALS

- Thin-Set Mortar: ANSI A118.4, latex-portland cement type.

- Grout: ANSI A118.6, polymer modified unsanded for joints 1/8 inch and smaller.

- Color: As selected by Architect from manufacturer's standard colors.

- Sanded grout for joints greater than 1/8 inch.

- Waterproof Membrane: ANSI A118.10, liquid-applied type for wet areas.

PART 3 - EXECUTION

- EXAMINATION

- Verify substrates are ready for tile installation:

- Surfaces are clean, dry, and free of contaminants.

- Concrete is cured minimum 28 days.

- Floor flatness meets requirements of TCNA Handbook.

- Do not proceed until unsatisfactory conditions are corrected.

- PREPARATION

- Prepare substrates per TCNA Handbook and setting material manufacturer's requirements.

- Apply waterproof membrane in wet areas:

- Toilet room floors and walls to 6 feet above floor.

- Shower walls full height.

- Lap seams minimum 2 inches.

- Lay out tile work to minimize cuts and maintain symmetry.

- INSTALLATION

- Install tile per TCNA Handbook method appropriate for substrate and application.

- Set floor tile with full mortar coverage.

- Set wall tile with minimum 80 percent coverage.

- Full coverage at wet areas.

- Full coverage at tile edges.

- Joint Width: 1/8 inch unless otherwise indicated.

- Grout joints after mortar has cured minimum 24 hours.

- Tool joints to uniform depth.

- Clean excess grout from tile surfaces before grout sets.

- Seal grout joints with penetrating sealer after grout has cured.

END OF SECTION